## Slide 1
Predicting Vibrational Mean Free Paths in Disordered Systems
Jason Larkin and Alan McGaughey
Department of Mechanical Engineering
Carnegie Mellon University, Pittsburgh PA
Massoud Kaviany Symposium
2013 Summer Heat Transfer Conference
July 16, 2013
Support: AFOSR

## Slide 2: Amorphous Solids
Experimental data from Touloukian, Thermophysical Properties of Matter.
Structural disorder
Composition disorder possible
Amorphous silicon (a-Si) and silica glass (a-SiO2)

## Slide 3: Mechanism?
Shenogin et al., JAP 105 (2009) 034906.
But, from classical MD:
FDTR Experiments (Malen):
  Regner et al., Nat. Comm. 4, 1640 (2013).

## Slide 4: Vibrational Modes in Disordered Systems
Extended modes
  Propagon (phonon-like)
  Diffuson (non-propagating, group velocity not well-defined)
Localized modes
  Locons (not relevant to 3-D thermal transport)
Classify using eigenvectors, other methods …
All modes have a lifetime → decay of their energy.

## Slide 5: Thermal Conductivity Prediction
PROPAGONS
DIFFUSONS
Allen and Feldman, PRB 48, 12581 (1993)

## Slide 6: Amorphous Structures
Amorphous silica (a-SiO2)
  BKS potential
  Melt-quench-anneal from quartz
  4608 Atoms
Amorphous silicon (a-Si)
  Stillinger-Weber potential
  WWW structures + anneal
  4096 Atoms
  a-Si: Barkema and Mousseau, PRB 62, 4985 (2000).
  a-SiO2: McGaughey and Kaviany, IJHMT 47, 1799 (2004).

## Slide 7: Computational Tools
Lattice dynamics theory
  Harmonic (frequencies, Allen-Feldman diffusivities)
Molecular dynamics simulation
  No assumptions about thermal transport (propagons vs. diffusons)
  Classical statistics
  Phonon lifetimes from normal mode decomposition
  Thermal conductivity from Green-Kubo method

## Slide 8: Treat Disorder Explicitly
Lattice dynamics only at the Gamma-point.
1 wave vector × 3N polarizations = 3N modes
Cannot specify group velocity.
He et al., APL 98, 144101 (2011),
Hori et al., JAP 113, 203514 (2013)
N atoms
Supercell = Unit Cell

## Slide 9: Green-Kubo Thermal Conductivity (Top-down)
  a-SiO2
  a-Si

## Slide 10: Bottom-Up Thermal Conductivity Prediction
Challenges:
  Where is the transition between propagons and diffusons?
  How to specify the propagon group velocity?
  How to include low-frequency modes not in MD?

## Slide 11: Density of States
Extract a single velocity scale from Debye region.
  a-SiO2
  a-Si

## Slide 12: Lifetimes
  a-SiO2
  Almost all diffusons.
  a-Si
  Clear propagon to diffuson transition.

## Slide 13: Challenges Addressed
How to specify the propagon group velocity?
  One velocity scale from DOS
Where is the transition between propagons and diffusons?
  Transition in t vs. w plot
How to include low-frequency modes not in MD?
  Summation → Integral

## Slide 14: Thermal Conductivity
  a-SiO2
  a-Si

## Slide 15: Thermal Conductivity Accumulation
  a-SiO2
  Mean Free Path, m
  a-Si
  Mean Free Path, m
  Regner et al., Nat. Comm. 4, 1640 (2013).

## Slide 16: Summary
Not all amorphous materials are alike
In a-SiO2, majority of thermal conductivity from diffusons
In a-Si, contributions from propagons and diffusons
Challenges in interpreting a-Si data due to range of experiments

## Slide 17: a-Si [100] Structure Factor and Dispersion

## Slide 18: a-SiO2 [100] Structure Factor and Dispersion

## Slide 19: Normal Mode Decomposition
1. Equilibrium MD simulations provide atomic velocities.
2. Project velocities onto phonon modes from lattice dynamics calculations.
3. Auto-correlation and Fourier transform of phonon kinetic energy.
4. Extract phonon lifetime.
  Ladd et al., PRB 34, 5068 (1986),
  McGaughey and Kaviany, PRB 69, 094308 (2004).

## Slide 20: Diffusivities
  a-SiO2
  a-Si

## Slide 21: Group Velocity from Gamma Analysis?
All modes have zero group velocity
at the Gamma-point.
1. Linear fit near Gamma-point
2. Gamma-X linear fit
He et al., APL 98, 144101 (2011)
Hori et al., JAP 113, 203514 (2013)